## Slide 1
Workshop: the DH&HML package
Chuhong Lin, PhD.
Research Fellow
School of Chemistry, Chemical Engineering and Biotechnology, Nanyang Technological University, Sinagpore

## Slide 2
Acknowledgements
Funding
High Performance Computing
This research was partially performed on resources of the National Supercomputing Centre, Singapore (https://www.nscc.sg).
Low Carbon Energy Research Funding Initiative, U2102d2013

## Slide 3
About Me
“University of Catford”
“Nanyang Catnological University”
Doctor of Philosophy in Physical and Theoretical Chemistry
University of Oxford, UK
Research Fellow
Nanyang Technological University, Singapore
Research focus: Investigating the influence of non-catalytic factors on electrochemical reactions by multiscale kinetics simulation.
Research focus: Catalyst design for the dehydrogenation of liquid organic hydrogen carriers by machine learning and first principle computation.

## Slide 4
These are also the obstacles that we are facing in catalyst design, especially for the heterogeneous catalytic reactions of large, organic molecules.
If AI can design logos, can they also design catalysts?
Practice to train your own machine learning models and calculate reaction kinetics.
Apply the DH&HML model to other dehydrogenation or hydrogenation reactions.
Goals of study
Understand the design principles of the DH&HML package.

## Slide 5
What is the DH&HML package?
Dehydrogenation/hydrogenation (DH&H) is to remove/add hydrogen from the reactant molecule.
DH
H
Synthesis of pharmaceuticals and fine chemicals
Applications
Fuel production
Hydrogen transport and storage
Chem. Rev. 2020, 120, 20, 11370-11419
Acc. Chem. Res. 2017, 50, 1, 74-85
Vitamin C

## Slide 6
Methyl cyclohexane
MCH, C7H14
Toluene
TOL, C7H8
Example reaction
Computational Chemistry
Reaction Kinetics Modelling
Catalyst Screening
Catalyst design by computational method
High-throughput calculation for complex reactions
Reaction energies
Reactivity and selectivity
Composition, structure, etc.
Accelerated by machine learning
Complex adsorption interaction  many affecting factors
Expensive data collection cost
Challenges
Pt nanoclusters
Adding promoters: M
Pt-M bimetallic nanoclusters

## Slide 7
What is included in the DH&HML package?
Two folders: 1) adsorption energy (ΔEads) prediction by machine learning (ML);
2) catalyst screening by ML predicted energy + microkinetic modelling (MKM)
Reactivity (Turnover frequency per site)
Selectivity (Surface coverage of intermediates)
ML folder
MKM folder
ΔEads
6 reaction intermediates
1
Calculating reaction kinetics
2
Mapping over different Pt-M nanoclusters
3
(ML: Machine Learning)
(MKM: Microkinetic Modelling)
Install MATLAB

## Slide 8
Data collection
Feature selection
Gaussian process regression
Active learning
Training data structure
Practice: training a GPR model
Machine learning
Microkinetic simulation
Content
Calculation of reaction rate constants
Application of ML model on MKM
Reaction rate equations
Activation barrier estimation
Numerical simulation
Validation
Practice: calculate TOF for a new catalyst
Homework: train a GPR model to predict the adsorption energy of C7H13.
Homework: screen over Pt-Ag nanoclusters.

## Slide 9
Parameter fitting
Validation and testing
Goal of the ML model: ΔEads prediction over different Pt-M bimetallic nanoclusters
Design principle of the DH&HML package I. Machine learning
ML model training
ML model
Input: Structure
Output: Adsorption energy
Information of adsorbate and catalyst
Training data collection
Both input and output from Density Functional Theory (DFT) calculation.
Feature selection
Numbers to represent the input information.
Suitable ML algorithm and the parameters or hyperparameters involved.
No overfitting, accuracy, generality, transferability, etc.

## Slide 10
Training data collection
DFT computation:
ΔEads
+
optimised structure
As many variables as possible (Generality)
As less calculation as possible (Cost)
Pt-M bimetallic nanoclusters
Material space
CUBO
55 atoms
DEC
55 atoms
4-fold (100)
3-fold
(111)
2-atoms
edge
Nanoparticle morphologies (global)
Active site (local)
OCT
44 atoms
Composition
Active site geometry
Facet
Coordination environment
Morphology
Size
Use the adsorption energy of toluene as an example.
Single adsorbate  easier to build an accurate model
Toluene  the most important intermediate (selectivity and reactivity)
TOL adsorbed on Pt55

## Slide 11
Data collection
1) Manually sampling over the high-dimensional material space, e.g. 5 compositions * 5 site geometry *...
2) Active learning: efficient mapping over the high-dimensional material space
Empirical data sampling design: using our chemical knowledge to decide the weight of each variable
MAE: mean absolute error
Uncertainty: Uncertainty of a prediction
~ Confidence interval of a normal distribution
Higher uncertainty  add the new data to the training dataset
uncertainty
Data with high uncertainty
Training data pool
ML model (GPR)
New testing data
MAE < 0.15 eV
Initial data collection
GPR: Gaussian Process Regression
DFT

## Slide 12
ML folder
Data_DFT folder stores all the DFT calculated data in the MCH-TOL project.
RandomDopedPt55 folder stores 131 pairs of data.
DFT calculation: Quantum ESPRESSO
Structure file: .xyz file  easy to operate by MATLAB
index_name of the NC.xyz
Bare nanoclusters
TOL adsorbed nanoclusters
index_TOL.xyz
The data in the Data_DFT folder are collected by manual sampling, not by active learning.

## Slide 13
Feature selection
What atomic properties affect the adsorption energy most significantly?
1) Physics-inspired feature selection: determining features based on our understanding
ΔEads
ML
How to present this structure by a vector of numbers?
Requirement of features/descriptors
Relevance
Uniqueness
Simplicity
Generalization Ability
Better explainability
Smaller dataset size requested

## Slide 14
Physics-inspired feature selection: knowledge from literatures on chemisorption
How many atoms should be taken into consideration?
Active site
(the atoms directly interacting with the adsorbate)
1st nearest neighbours
(the atoms attaching with the active site atoms)
Which atomic properties are correlated with chemisorption?
Cohesive energy
Electronegativity
Coordination number
Bond information
J. Phys. Chem. Lett. 10, 1852–1859 (2019)
ACS Catal. 13, 13663–13671 (2023)
ACS Catal. 14, 874–885 (2024)
Nat. Commun. 11, 1196 (2020)
ACS Catal. 2, 12–16 (2012)
Adv. Sci. 10, 2207644 (2023)

## Slide 15
Using individual properties may not give the optimal prediction performance.
For alloys, we need to represent the ligand effect.
Pt-M: for each metal, the ligand metal atoms around it may not be the same as the host metal atom, which causes a d-orbital shift of the host metal.
Pt55: all metal atoms are Pt.
The d-orbital shift was regarded as the primary cause of changes in chemisorption due to ligand effects.
Chem 6.11 (2020): 3100-3117
J. Chem. Phys. 120, 10240–10246 (2004)
Each Pt-M bimetallic nanocluster  a unique [F1, F2, F3] fingerprint vector
nas: the number of active site

## Slide 16
ΔEads, GPR (eV)
Uncertainty
(2.18, -2.96)
dC-Pt/M ()
Minimal uncertainty point is regarded as the prediction result.
DFT calculation: 2.16 Å and –2.89 eV
Cohesive energy Ecoh and electronegativity χ are all collected from database/textbooks.
Coordinate number is calculated from the nanoparticle morphology.
For training data, the average bond length is obtained from DFT optimised .xyz file.
But for testing data, this property is treated as an variable, from 2 to 3 Å.

## Slide 17
2) Automatic feature selection: Symbolic regression, e.g. SISSO.
List all the possible atomic properties: electronegativity, element number, atomic radius, etc.
Determine the most correlated properties
+
Provide the mathematical expression of descriptors
Phys. Rev. Materials, 2, 083802

## Slide 18
Gaussian process regression
Parameter fitting
 | F1 | F2 | F3
1 |  |  | 
2 |  |  | 
… |  |  | 
131 |  |  | 
Input x: 131 data * 3 features
Input y: 131 ∆Eads
y = GPR(x)
GPR model
MATLAB built-in function: fitrgp
How to evaluate the performance of the model:
Small error
High correlation
Not overfitted
Transferable

## Slide 19
131 data points
5-fold validation
80%: Training
20%: Testing
This is the function to call when you want to train a GPR model.

## Slide 20
Transferability testing
a
Doping index increases
...
Change elements
ΔEads, TOL(eV)
b
Period 3
Period 4
Period 5
: used in training data
M
M
: new element
Au
Cd
Ti
Co
Pb
MAE = 0.19 eV
GPR model  New data

## Slide 21
ML folder
Training data from DFT calculation
Fingerprints of the training dataset
GPRModel_Fcn is used to train a GPR model.
Practice: How to train a GPR model predicting adsorption energy
Visualization_Fcn is used to view a .xyz file.
Use class SingleData and EnsembleData to extract features and generate fingerprints
Edit these functions when you want to change the criterion and definitions of features and fingerprints.
Scripts to use the above functions to convert .xyz files into fingerprints and train a GPR model.

## Slide 22
Dual-site assumption: C7Hx* and HΔ occupy different sites
H-H recombination is relatively faster than other reactions.
A* + Δ = B* + HΔ
Non-linear ordinary differential equation (ode)
x7
x2
Design principle of the DH&HML package II. Microkinetic model
Continuous stirred-tank reactor

## Slide 23
Calculate reaction rate constants from DFT calculated energies
Adsorption-desorption
Collision theory
Equilibrium constant
Transition state theory
Surface reaction
A* + Δ = B* + HΔ
∆G : reaction energy
∆G = Gproducts – Greactants
∆Gact : activation barrier
∆Gact = Gtransition state - Greactants
a: active site area (m2)
M: molecule mass (kg)
kB: the Boltzmann constant
(1.38x10-23 J/K)
T: temperature
R: the gas constant
(8.314 J/mol/K)
A + * = A*
Chem. Rev. 2021, 121, 1049−1076

## Slide 24
A + * = A*
(*: Pt-M site)
GPR model prediction
k = function(∆G, ∆Gact )
?
Adsorption-desorption
Zero-point energy (ZPE): the ground state energy.
Surface reaction
A* + Δ = B* + HΔ
ΔEZPE, A-B is E­ZPE,B* – EZPE,A* – EZPE,HΔ and ΔSA-B is SB* - SA* - SHΔ.
k = function(∆G , ∆Gact )
ZPE and S are assumed to be independent of active site composition in the simulation.
+
H adsorption energy is assumed to be independent of active site composition.
DFT-calculated ZPE and S terms
DFT-calculated reference active site on Pt55 (4-fold site on the 100 facet)
GPR model
∆Eads terms

## Slide 25
We assumed that the transition state’s ZPE and S are also independent of the active site composition.
Constant term for a given A  B step, calculated once via DFT on the reference site.
Brønsted−Evans−Polanyi (BEP) Relation
a, b are coefficients, which can be fitted from the six C-H breakage steps calculated on the reference active site.
k = function(∆G, ∆Gact)
DFT-calculated reference active site on Pt55 (4-fold site on the 100 facet)
GPR model
+
BEP relation
+
rate, θ

## Slide 26
Pt55 nanocluster
Transition states
Reaction intermediates
Pt(100) facet
Temperature: 600 K
Pressure: 1 bar (MCH)
DFT calculated free energy diagram
ML model  E, enthalpy
G = E – T*S
T: temperature
S: entropy
Entropy of gas-phase molecules: Ideal gas assumption
Entropy of adsorbates: Harmonic limit
https://wiki.fysik.dtu.dk/ase/ase/thermochemistry/thermochemistry.html
Quantum ESPRESSO + Atomic Simulation Environment (ASE)
Reaction rate constants k
Gibbs free energy G

## Slide 27
Numerical simulation: Finite difference method
x7
x2
Numerical simulation: Self-consistent pH2
pH2 = 0
Odes of C7Hx
pH2 = 3*pTOL
No

## Slide 28
Validation
Analytical reaction rate expression when TOL desorption is the only rate-determining step:
rate = kTOL,des
Quasi-equilibrium adsorption
Steady state
(user-defined criterion)
A + * = A*

## Slide 29
Practice: How to use the GPR models to screen catalysts for MCH dehydrogenation?
MKM folder
Vibration frequencies calculated from DFT computation
.xyz files for reaction intermediates on the reference Pt55
Function used to calculate ΔG and ΔGact
Function using ΔG and ΔGact to calculate reaction kinetics
Trained GPR models for each reaction intermediates from C7H13 to C7H8.